Copyright 2014 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

This Product MasterSpec Section is licensed by ARCOM to Everkem Diversified Products, Inc. ("Licensee").

This Product MasterSpec Section modifies the original MasterSpec text and does not include the full content of the original MasterSpec Section.

Revisions made to the original MasterSpec text are made solely by the Licensee and are not endorsed by, or representative of the opinions of, ARCOM or The American Institute of Architects (AIA). Neither AIA nor ARCOM are liable in any way for such revisions or for the use of this Product MasterSpec Section by any end user. A qualified design professional should review and edit the document to suit project requirements.

For more information, contact Everkem Diversified Products, Inc., 5180 Indiana Ave., Winston-Salem, NC 27106; Phone: (800) 638-3160; Fax: (336) 661-7969; Website: www.everkemproducts.com.

For information about MasterSpec, contact ARCOM at (800) 424-5080 or visit www.MasterSpec.com.

SECTION 079219 - ACOUSTICAL JOINT SEALANTS

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

GENERAL

RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

SUMMARY

Section includes acoustical joint sealants.

Related Requirements:

Retain subparagraph below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

Section 079200 "Joint Sealants" for elastomeric, latex, and butyl-rubber-based joint sealants for nonacoustical applications.

ACTION SUBMITTALS

Product Data: For each acoustical joint sealant.

Sustainable Design Submittals:

"Product Data" Subparagraph below applies to LEED 2009 NC, CI, and CS; LEED v4; IgCC; ASHRAE 189.1; and Green Globes. Coordinate with requirements for sealants.

Product Data: For sealants, indicating VOC content.

"Laboratory Test Reports" Subparagraph below applies to LEED 2009 for Schools, LEED v4, IgCC, ASHRAE 189.1, and Green Globes. Coordinate with requirements for sealants.

Everkem's "SoundSeal 90" is currently undergoing third-party testing.

Laboratory Test Reports: For sealants, indicating compliance with requirements for low-emitting materials.

Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs below for two-stage Samples.

Samples for Initial Selection: Manufacturer's color charts consisting of strips of cured sealants showing the full range of colors available for each product exposed to view.

Samples for Verification: For each kind and color of acoustical joint sealant required, provide Samples with joint sealants in 1/2-inch- (13-mm-) wide joints formed between two 6-inch- (150-mm-) long strips of material matching the appearance of exposed surfaces adjacent to joint sealants.

Acoustical-Joint-Sealant Schedule: Include the following information:

Joint-sealant application, joint location, and designation.

Joint-sealant manufacturer and product name.

Joint-sealant formulation.

Joint-sealant color.

INFORMATIONAL SUBMITTALS

Product Test Reports: For each kind of acoustical joint sealant, for tests performed by [manufacturer and witnessed by a qualified testing agency] [a qualified testing agency].

Sample Warranties: For special warranties.

DELIVERY, STORAGE, AND HANDLING

Deliver materials undamaged in manufacturer's clearly labeled, unopened containers.

Coordinate delivery of materials with scheduled installation date to allow minimum storage time at Project site.

Store materials under cover and protect from weather and damage in compliance with manufacturer’s requirements. Comply with recommended procedures, precautions, or remedies.

Do not use damaged or expired materials.

FIELD CONDITIONS

Apply acoustical sealant only when temperature of substrate surface and ambient air temperatures are between 50 and 95 deg F (10 and 35 deg C).

Do not apply acoustical sealant in snow, rain, fog, or mist, when relative humidity exceeds 85 percent; at temperatures less than 5 deg F (3 deg C) above the dew point, or to damp or wet surfaces.

WARRANTY

When warranties are required, verify with Owner's counsel that special warranties stated in this article are not less than remedies available to Owner under prevailing local laws.

Installer's Special Warranty: Installer agrees to repair or replace acoustical joint sealants that fail in materials or workmanship within specified warranty period.

Verify available warranties and warranty periods for acoustical joint-sealant installation.

Warranty Period: [Two] <Insert number> years from date of Substantial Completion.

Manufacturer's Special Warranty: Manufacturer agrees to repair or replace acoustical joint sealants that fail in materials or workmanship within specified warranty period.

Verify available warranties and warranty periods for acoustical joint sealants.

Warranty Period: Five  years from date of Substantial Completion.

PRODUCTS

Manufacturers and products listed in SpecAgent and MasterWorks Paragraph Builder are neither recommended nor endorsed by the AIA or ARCOM. Before inserting names, verify that manufacturers and products listed there comply with requirements retained or revised in descriptions and are both available and suitable for the intended applications. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

PERFORMANCE REQUIREMENTS

Provide acoustical joint-sealant products that effectively reduce airborne sound transmission through perimeter joints and openings in building construction, as demonstrated by testing representative assemblies according to ASTM E 90.

Subparagraph below applies to LEED 2009 NC, CI, and CS; LEED v4; IgCC; ASHRAE 189.1; and Green Globes.

Sealant shall have a VOC content of 250 g/L or less.

Subparagraph below applies to LEED v4.

Everkem's "SoundSeal 90" is currently undergoing third-party testing.

Sealant shall comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

Retain “Surface-Burning Characteristics” Paragraph below when required.

Surface-Burning Characteristics: Comply with ASTM E 84; testing by a qualified testing agency. Identify products with appropriate markings of applicable testing agency.

Retain “Mold and Mildew Resistance” Paragraph below when required.

Mold and Mildew Resistance: Zero (0) or “no growth” in accordance with ASTM G 21.

ACOUSTICAL JOINT SEALANTS

Acoustical Sealant for Exposed and Concealed Joints: Manufacturer's standard nonsag, paintable, nonstaining latex acoustical sealant complying with ASTM C 834.

Basis-of-Design Product: Subject to compliance with requirements, provide Everkem Diversified Products, Inc.; SoundSeal 90 Draft, Smoke, & Acoustical Sound Sealant or a comparable product by one of the following:

GE Construction Sealants; Momentive Performance Materials Inc.

Pecora Corporation.

Tremco Incorporated.

<Insert manufacturer's name>.

Colors of Exposed Acoustical Joint Sealants: As indicated by manufacturer's designations <Insert color>.

VOC content of 24.7 g/L below, for Everkem's "SoundSeal 90 Draft, Smoke, & Acoustical Sound Sealant," complies with VOC requirements for LEED 2009 NC, CI, and CS; LEED v4; IgCC; ASHRAE 189.1; and Green Globes.

VOC Content: 24.7 g/L or less.

MISCELLANEOUS MATERIALS

Cleaners for Nonporous Surfaces: Chemical cleaners acceptable to manufacturers of sealants and sealant backing materials, free of oily residues or other substances capable of staining or harming joint substrates and adjacent nonporous surfaces in any way, and formulated to promote optimum adhesion of sealants to joint substrates.

Masking Tape: Nonstaining, nonabsorbent material compatible with joint sealants and surfaces adjacent to joints.

EXECUTION

EXAMINATION

Examine joints indicated to receive acoustical joint sealants, with Installer present, for compliance with requirements for joint configuration, installation tolerances, and other conditions affecting performance of the Work.

Proceed with installation only after unsatisfactory conditions have been corrected.

PREPARATION

Surface Cleaning of Joints: Clean out joints immediately before installing acoustical joint sealants to comply with joint-sealant manufacturer's written instructions.

Masking Tape: Use masking tape where required to prevent contact of sealant or primer with adjoining surfaces that otherwise would be permanently stained or damaged by such contact or by cleaning methods required to remove sealant smears. Remove tape immediately after tooling without disturbing joint seal.

INSTALLATION OF ACOUSTICAL JOINT SEALANTS

For application procedures, refer to Everkem's “Technical Data Sheet” document link at www.everkemproducts.com/wp-content/uploads/2014/01/SoundSeal90_Acoustical-Sound-Sealant_Technical-Data-Sheet.pdf.

Comply with acoustical joint-sealant manufacturer's written installation instructions unless more stringent requirements apply.

Install acoustical sealant, free of air pockets, embedded foreign matter, sags, and ridges.

Tooling of Nonsag Sealants: Immediately after sealant application and before skinning or curing begins, tool sealants to form smooth, uniform beads to eliminate air pockets and to ensure contact and adhesion of sealant with sides of joint.

Remove excess acoustical sealant from surfaces adjacent to joint.

Use tooling agents approved by sealant manufacturer that do not discolor sealants or adjacent surfaces.

Retain "STC-Rated Assemblies" and "Acoustical Ceiling Areas" paragraphs below as required, or revise to include additional applications to suit Project.

STC-Rated Assemblies: Seal construction at perimeters, behind control joints, and at openings and penetrations with a continuous bead of acoustical joint sealant. Install acoustical joint sealants at both faces of partitions, at perimeters, and through penetrations. Comply with ASTM C 919, ASTM C 1193, and manufacturer's written recommendations for closing off sound-flanking paths around or through assemblies, including sealing partitions to underside of floor slabs above acoustical ceilings.

Acoustical Ceiling Areas: Apply acoustical joint sealant at perimeter edge moldings of acoustical ceiling areas in a continuous ribbon concealed on back of vertical legs of moldings before they are installed.

FIELD QUALITY CONTROL

Inspection of Acoustical Joint Sealant Installation:

Inspect tested joints acoustical joints and penetrations to ensure proper installation before concealing or enclosing areas, and examine the following:

Whether sealant is free of voids and has filled joint cavities.

Whether sealant dimensions and configurations comply with specified requirements.

Whether sealants in joints fail to adhere to joint substrates or tear cohesively.

Repair sealants disturbed during inspection of area by applying new sealants following same procedures used originally to seal joints. Ensure that original sealant surfaces are clean and that new sealant contacts original sealant.

CLEANING

Clean off excess sealant or sealant smears adjacent to joints as the Work progresses by methods and with cleaning materials approved in writing by manufacturers of acoustical joint sealants and of products in which joints occur.

PROTECTION

Protect acoustical joint sealants during and after curing period from contact with contaminating substances and from damage resulting from construction operations or other causes so sealants are without deterioration or damage at time of Substantial Completion. If, despite such protection, damage or deterioration occurs, cut out, remove, and repair damaged or deteriorated acoustical joint sealants immediately so installations with repaired areas are indistinguishable from original work.

END OF SECTION 079219